M10	CEMENT BASED LEVELING / WEARING SCREEDS

To be read with Preliminaries / General conditions.

J40/310333333333

3100110101010293I8E4844444

140A 	PROPRIETARY POLYMER MODIFIED LEVELLING SCREEDS

- Substrate :  …………………

- Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-     Product reference : RIW Cementfill FC

- Screed construction : Fully bonded.

- Thickness :

-    Nominal : 3mm.

-    Minimum : 0mm.

-    Maximum : 6mm per layer.

- Mix :

-    Proportions : 6.5 parts powder to 1 part water, by volume.

- Primer : RIW Cementseal Primer

- Finish :  …………………

-    To receive …………………

- 	Other requirements …………………