J10	CEMENTITIOUS MORTAR TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES OF TANKING / DAMP PROOFING

J40/310333333333

3100110101010293I8E4844444

110A	CEMENTITIOUS MODIFIED POLYMER RICH COATING

- Substrate : …………………

- Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

- 	Product reference : RIW Cementflex

- Number of coats : Two

or : for floor coatings

- Number of coats : One

- Thickness : 2mm overall

- Primer : Not required

or : for horizontal surfaces

- Primer : RIW Cementseal Primer

- Finish : …………………

- Other requirements : …………………

- Joint tape : Not required

or

- Joint Tape : As Clause 330.

MATERIALS AND MAKING OF MORTAR

- MOVEMENT JOINT SYSTEM

- Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-	Product reference : RIW Cementjoint

-	Application : Embedded between two 1mm thick coats.

360	COLD WEATHER

-	General : Do not use frozen materials or apply coatings to frozen or frost-bound `		substrates.

-	Air temperature requirements : Do not apply coatings when at or below 5oC and falling, or below 3oC and rising.

-	Temperature of work : Maintain above 5oC until coatings have hardened.

PREPARING SUBSTRATES

J30/410A	SUITABILITY OF SUBSTRATES

-	Preparation generally : In accordance with RIW Limited’s recommendations.

-	Stability and soundness : Free from movement, and loose or weak areas that will cause failure of the tanking.

-	Key : To achieve firm adhesion of the tanking.

-	Contamination : Free from previous coatings and contaminants including laitance, dirt, dust, efflorescence, mould, oil, paint and plaster.

-	Cracks, porous patches and other defective areas subject to water pressure and liable to admit water : Control and seal using RIW Cementfill WP in accordance with RIW Limited’s recommendations.

J30/420A	PREPARATION OF MORTAR JOINTS AND CAVITIES

-	Mortar joints : Rake out to a depth of 12mm minimum.

- 	Debris : Remove and flush out with water.

-	Fill : Repoint with RIW Cementfill HB in accordance with RIW Limited’s recommendations.

-	Blow holes, cavities, cracks, etc. : Remove loose material and fill flush using RIW Cementfill FC  in accordance with RIW Limited’s recommendations.

430	TANKING INTEGRITY

-	Penetrations for fixings, services, etc. : Not permitted.

EXECUTION

J30/510A	APPLICATION GENERALLY

- Application methods : Substrate surfaces are to be thoroughly soaked with clean            	water until uniformly saturated without standing water, prior to application.

J30/520	JOINTS / JUNCTIONS AND PENETRATIONS

- Abutments, joints and active cracks : Sealed and watertight.

- 	Movement joints : Centred over joints in substrate and extended through waterproof coating and finishes .

-	Daywork joints in successive coatings : Staggered and lapped.

-	Angled joints : Not permitted.

-	Penetrations : Watertight.

530	APPEARANCE OF TANKING

- 	Render / Screed coatings : Even and consistent. Free from rippling, hollows, ridges, cracking and crazing.

-	Accuracy : A true plane, to correct line and level. Walls and reveals plumb and square with neat arrises.

-	Thin slurry coatings : Consistent and free from hollows, cracks and crazing. Suitable to receive specified finish.

550A	CURING AND DRYING

-	General : Prevent premature setting, uneven drying and cracking of each coat.

-	Curing coatings : Prevent evaporation from surface by the use of RIW Cementseal Primer.

-	Curing Period : Normally overnight ; temperature dependent.

560	PROTECTION

-	Mechanical damage : Prevent impact and abrasion.

-	Application of protective coatings / linings : After completion of curing.