C42	REPAIRING / RENOVATING / CONSERVING  CONCRETE

To be read with Preliminaries / General conditions.

J40/310333333333

3100110101010293I8E4844444

310A	REPAIR MORTAR

- Type : Modified polymer rich cementitious coating

- Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-     Product reference : RIW Cementflex

- Number of coats : Two

- Thickness per coat : 1mm vertical

- Primer : Not required.

or : for horizontal surfaces

- Number of coats : One

- Thickness per coat : 2mm

- Primer : RIW Cementseal Primer.