J40	FLEXIBLE SHEET TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES OF TANKING / DAMP PROOFING

J40/295 	GEOCOMPOSITE STUDDED CAVITY DRAINAGE / VENTING MEMBRANE

- Substrate :

- Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

- Product reference : RIW Double Drain.

- Stud height : 8mm.

- Fixing : RIW Adhesive Tape, unless noted otherwise.

-	     Fixing centres : 2000mm maximum.

- Joints : Separate geotextile fabric from studded sheet, make overlapped joint and connect in accordance with manufacturer’s recommendations.

- Exposed edges and corners : Seal with geotextile fabric to prevent silt entering the core.

- Accessories : RIW Top Edging Strip.

WORKMANSHIP

J40/310 A	WORKMANSHIP GENERALLY

- Condition of substrate :

-   	Clean and even textured, free from voids and sharp protrusions.

- Condition at completion :

-	Neat, smooth and fully supported, dressed well into abutments and around intrusions.

-	Completely continuous.

-	Undamaged. Prevent puncturing during following work.

- Permanent overlying construction: Cover as soon as possible.

J40/370 A	PIPES, DUCTS, CABLES, ETC :

- Where these pass through sheeting, follow details as recommended for the purpose by the sheet manufacturer.