J40	FLEXIBLE SHEET TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES OF TANKING / DAMP PROOFING

J40/297 	REINFORCED HIGH PERFORMANCE POLYETHYLENE DAMP PROOFING

- Substrate : …………………

-	Primer : Not required

-	Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-	Product reference : RIW DPM Red.

- Number of layers : One.

- Thickness / Gauge : 0.5mm / 2000g

- Joints :

-	Surfaces to be joined : Clean and dry beyond full width of joint.

-	Laps ( minimum ) : 150mm

-	Sealing : RIW Seal Tape between overlaps, edge of top sheet sealed with RIW Lap Tape.

WORKMANSHIP

J40/310	WORKMANSHIP GENERALLY

- Condition of substrate :

-	Clean and even textured, free from voids and sharp protrusions.

-	Moisture content : Compatible with damp proofing / tanking.

- Air and surface temperature : Do not apply sheets if below minimum recommended by sheet manufacturer.

- Condition of membrane at completion :

-	Neat, smooth and fully supported, dressed well into abutments and around intrusions.

-	Completely impervious and continuous.

-	Undamaged. Prevent puncturing during following work.

- Permanent overlying construction : Cover membrane as soon as possible.

J40/320	INSPECTION

- Give notice : Before covering any part of membrane with overlying construction.

J40/360	JUNCTIONS WITH PROJECTING DPC’S / CAVITY TRAYS

- Adjoining surfaces : Clean and dry.

- DPC’s / cavity trays : Lap and fully bond / seal with sheeting.

-	Laps ( minimum ) : 100mm.

-	Bonding / Sealing : As main sheeting.

J40/370A	PIPES, DUCTS, CABLES, ETC

- Where these pass through sheeting, make junctions completely impervious using preformed collars as supplied by sheeting manufacturer.

or

- RIW Sheetseal 226 in accordance with the data sheet for the product.