J30	LIQUID APPLIED TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES OF TANKING / DAMP PROOFING

J30/110 	COLD APPLIED TANKING

-	Substrate : …………………

-	Primer : Not required.

-	Coating : Bituminous solution.

-	Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

- 	Product reference : RIW Liquid Asphaltic Composition (LAC).

-	Application : Number of coats : Two (2).

Coverage per coat (min) : 1.7m² / litre – 1st coat, 2.5m² / litre – 2nd coat.

-	Reinforcement : RIW Sheetseal 226 x 300mm wide.

EXECUTION

J30/205A 	SUITABILITY OF SUBSTRATE

-	Substrates generally :

-	Smooth, even textured, clean, dry and frost free.

-	Within tolerances for level and surface regularity.

-	Vertical and horizontal surfaces : Correctly prepared and free from irregularities.

-	Moisture content and stability of substrate : Must not impair integrity of finished tanking / damp proofing.

-	Preliminary work : Complete including :

-	Chases.

-	External angles.

-	Formation of upstands and kerbs.

-	Movement joints.

-	Penetrations / Outlets.

J30/210 	COATING APPLICATION

-	Adjacent surfaces exposed to view in finished work : Protect.

-	Coatings :

- Apply in dry atmospheric conditions, when substrate is dry.

- Uniform, continuous coverage. Do not allow to pool in hollows.

-	Firmly adhered to substrate and free from imperfections.

-	Prevent damage to finished coatings.

-	Penetrations: Impervious.

-	Final covering: Apply as soon as possible after coating has hardened.

J30/220	COLD APPLIED COATINGS

-	Thinning : Not permitted unless recommended by manufacturer.

-	Successive coats :

-	Allow to dry before applying next.

-	Apply at right angles to previous.

J30/230 	BITUMINOUS COATINGS

-	Air and surface temperatures (minimum) : 5°C.

-	Weather conditions : Do not apply if there is a risk of rain during application and drying, unless effective temporary cover is provided over working area.

- Unavoidable wetting of construction or coating : Minimize and make good damage.

J30/240	REINFORCEMENT

-	Laying : When RIW Liquid Asphaltic Composition is dry.

-	Edge overlap (minimum) : 150mm either side of joint.

-	Finish : Smooth and free from imperfections.

COMPLETION

J30/330	PROTECTION OF COATINGS

-	Coated surface : Clean and free from contaminants.

-	Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-	Product reference : Double Drain

-	Thickness : 8mm.

-	Placement : Bond to coating with RIW Adhesive Tape.

-	Edge overlap (minimum) : 70mm.

-	Perimeter treatment : Seal with geotextile fabric to  prevent silt entering the core.

-	Contact  with coating : Secure and continuous.

or

-	Product reference : RIW Protection Board.

-	Thickness : 3mm.

-	Placement : Bond to coating with RIW Adhesive Tape.

-	Edge overlap (minimum) : Not required.

-	Perimeter treatment : Butt joint.

-	Contact with coating : Secure and continuous.

340	BACKFILLING TO EXTERNAL COATINGS

-	Timing : Carry out as soon as possible after tanking and protection are complete.