J30	LIQUID APPLIED TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES OF TANKING / DAMP PROOFING

J30/130 	COLD APPLIED DAMP PROOFING

-	Substrate : ………………...

-	Primer : Not required.

-	Coating : Bitumen solution.

-	Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-	Product reference : RIW Liquid Asphaltic Composition ( LAC ).

-	Application : Number of coats : Two ( 2 ).

Coverage per coat (min) : 1.7m² / litre – 1st coat, 2.5m² / litre – 2nd coat.

-	Reinforcement : RIW Sheetseal 226 x 150mm wide.

-	Blinding : Not required.

EXECUTION

J30/205A 	SUITABILITY OF SUBSTRATE

-	Substrates generally :

-	Smooth, even textured, clean, dry and frost free.

-	Within tolerances for level and surface regularity.

-	Vertical and horizontal surfaces : Correctly prepared and free from irregularities.

-	Moisture content and stability of substrate : Must not impair integrity of finished tanking / damp proofing.

-	Preliminary work : Complete including :

-	Chases.

-	External angles.

-	Formation of upstands and kerbs.

-	Movement joints.

-	Penetrations / Outlets.

J30/210 	COATING APPLICATION

-	Adjacent surfaces exposed to view in finished work : Protect.

-	Coatings :

- Apply in dry atmospheric conditions, when substrate is dry.

- Uniform, continuous coverage. Do not allow to pool in hollows.

-	Firmly adhered to substrate and free from imperfections.

-	Prevent damage to finished coatings.

-	Penetrations: Impervious.

-	Final covering: Apply as soon as possible after coating has hardened.

J30/220	COLD APPLIED COATINGS

-	Thinning : Not permitted unless recommended by manufacturer.

-	Successive coats :

-	Allow to dry before applying next.

-	Apply at right angles to previous.

J30/230 	BITUMINOUS COATINGS

-	Air and surface temperatures (minimum) : 5°C.

-	Weather conditions : Do not apply if there is a risk of rain during application and drying, unless effective temporary cover is provided over working area.

- Unavoidable wetting of construction or coatings : Minimize and make good damage.

J30/240	REINFORCEMENT

-	Laying : When Liquid Asphaltic Composition is dry.

-	Edge overlap (minimum) : 75mm either side of joint.

-	Finish : Smooth and free from imperfections.

J30/260	JUNCTIONS WITH DPCs

-	DPC’s : Clean, all edges fully exposed.

- Application : Fully coat DPC, and overlap adjacent surfaces by (minimum) 75mm.