J40	FLEXIBLE SHEET TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES  OF  TANKING / DAMP  PROOFING

J40/285A 	LOOSE LAID BENTONITE DAMP PROOFING / TANKING

- Substrate : …………………

- Primer : Not required.

-	Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

- 	Product reference : RIW Structureseal.

- Number of layers : One.

- Laying : Staggered joints.

- Fixing to vertical / sloping surfaces : RIW Washers as required, to suit background.

- Fixings for horizontal surfaces : RIW Staples at 400mm maximum centres.

- Joints : Lapped minimum 100mm.

-	Sealing : Not required.

- Accessories : RIW Sealing Compound & RIW Granules.

RIW Waterstop, as Specification E40, Clause 320.

WORKMANSHIP

J40/310	WORKMANSHIP GENERALLY

- Condition of substrate :

-	Clean and even textured, free from voids and sharp protrusions.

-	Moisture content : Compatible with damp proofing / tanking.

- Air and surface temperature : Do not apply sheets if below minimum recommended by sheet manufacturer.

- Condition of membrane at completion :

-	Neat, smooth and fully supported, dressed well into abutments and around intrusions.

-	Completely impervious and continuous.

-	Undamaged. Prevent puncturing during following work.

- Permanent overlying construction : Cover membrane as soon as possible.

J40/320	INSPECTION

- Give notice : Before covering any part of membrane with overlying construction.

J40/370A	PIPES, DUCTS, CABLES, ETC :

- Where these pass through sheeting, make junctions completely impervious using a 40 x 40mm fillet of RIW Sealing Compound, applied over the RIW Structureseal.