J40	FLEXIBLE SHEET TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES OF TANKING / DAMP PROOFING

J40/180  	SELF - ADHESIVE BITUMEN GAS RETARDANT DAMP PROOFING / TANKING

- Substrate : …………………

-     Primer : Required for vertical or inclined surfaces - As Clause 335.

-	Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-	Product reference : RIW Sheetseal GR.

- Number of layers : One.

- Thickness / Gauge : 1.5mm ( applied ).

- Bonding : Full. Smooth out to exclude air.

- Joints :

- Surfaces to be joined : Clean and dry beyond full width of joint.

- Laps ( minimum ) :150mm.

- Sealing : Roll to fully adhere.

- Accessories : Not required

WORKMANSHIP

J40/310	WORKMANSHIP GENERALLY

- Condition of substrate :

-	Clean and even textured, free from voids and sharp protrusions.

-	Moisture content : Compatible with damp proofing / tanking.

- Air and surface temperature : Do not apply sheets if below minimum recommended by membrane manufacturer.

- Condition of membrane at completion :

-	Neat, smooth and fully supported, dressed well into abutments and around intrusions.

-	Completely impervious and continuous.

-	Undamaged. Prevent puncturing during following work.

- Permanent overlying construction : Cover membrane as soon as possible.

J40/320	INSPECTION

- Give notice : Before covering any part of membrane with overlying construction.

J40/335	PRIMERS

-	Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-	Product reference : RIW Sheetseal Primer.

- Coverage per coat ( minimum ) : 8m² / litre

- Curing : Allow to dry thoroughly before covering.

J40/350A	ANGLES IN BONDED DAMP PROOFING / TANKING

- Fit internal angles with a sand / cement fillet, not less than 40 x 40mm, unless noted otherwise.

- Reinforcing strip to all angles:

-	Material : As damp proofing / tanking.

-	Width ( minimum ) : 300mm.

-	Timing : Apply before main sheeting.

- Dressing of main sheeting onto adjacent surfaces ( minimum ) : 150mm.

J40/360	JUNCTIONS WITH PROJECTING DPC’S / CAVITY TRAYS

- Adjoining surfaces : Clean and dry.

- DPC’s / cavity trays : Lap and fully bond / seal with sheeting.

-	Laps ( minimum ) : …………………

-	Bonding / Sealing : …………………

J40/380A	PROTECTION BOARDS FOR DAMP PROOFING / TANKING

-	Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-	Product reference : RIW Protection Board

- Thickness : 3mm

- Application :

- Membrane surface : Clean and free from contaminants.

- Bonding : RIW Adhesive Tape.

- Board joints : Butted together.

- Board contact with membrane : Secure and continuous.

- Backfilling : Carry out as soon as possible after membrane and protection are complete.

or

- See Clause 295.